**Production of Diatomite Reinforced Polyester Composite and**

**Investigation of Its Thermophysical Properties**

***Mustafa DAĞ1 , Zehra Gülten YALÇIN1 , Ercan AYDOĞMUŞ2\* ***

*1Chemical Engineering,* *Engineering Faculty, Çankırı Karatekin University, Çankırı, Türkiye*

*2 Chemical Engineering, Engineering Faculty, Fırat University, Elazığ, Türkiye*

|  |
| --- |
|  **Abstract**In this study, composite materials have been improved by reinforcing diatomite soil into unsaturated polyester. Diatomite in the particle size range of 297 to 149 microns is used as a filler after drying at 105 °C. Diatomite reinforced polyester composites at different ratios by mass (0 %, 1 %, 3 %, 5 %, and 7 %) are produced at room temperature under open conditions to the atmosphere. In the experimental studies, the homogeneity of unsaturated polyester (UP) and the filler is provided first. Then, after methyl ethyl ketone peroxide (MEKP) and cobalt octoate (Co Oc) catalysts are added to the mixture, mixing is done at 1000 rpm for 2 min [1-3]. After the polyester composite is cured for 24 hours under laboratory conditions, necessary tests and analyzes are performed. The chemical bond structure of the obtained polyester composite is determined by Fourier transform infrared (FTIR) spectroscopy. The surface morphology of the composite material is examined by scanning electron microscopy (SEM). As the mass ratio of diatomite soil in the mixture raises, the porosity of the obtained composite increases. In the results, it has been observed that the density of the polyester composite decreases as the ratio of diatomite in the mixture by mass increases. Diatomite reinforcement changes the thermal conductivity coefficient of the polyester composite between 0.056 W/m·K and 0.079 W/m·K. Besides, Shore D hardness of the polyester composite varies between 78.0 and 81.5. It is observed that diatomite reinforcement tends to increase both the thermal conductivity and Shore D hardness of the polyester composite. Also, thermal decomposition experiments are carried out in a PID-controlled system in an inert environment between 25 °C and 605 °C. In the thermal decomposition experiments of polyester composites, it has been determined that the filler reinforcement increases the activation energy. Activation energy values are calculated using Coats-Redfern method when the temperature rise is 10 °C/min and the conversion rate (α) is between 0.1 and 0.9. Therefore, increasing the activation energy improves the thermal stability of the composite [4-6]. |
| Keywords: Diatomite, Polyester Composite, Density, Hardness, Thermal Conductivity |

**References**

1. Orhan, R., Aydoğmuş, E., Topuz, S., & Arslanoğlu, H. (2021). Investigation of thermo-mechanical characteristics of borax reinforced polyester composites. *Journal of Building Engineering*, 42, 103051.
2. Aydoğmuş, E., Arslanoğlu, H., & Dağ, M. (2021). Production of waste polyethylene terephthalate reinforced biocomposite with RSM design and evaluation of thermophysical properties by ANN. *Journal of Building Engineerin*g, 44, 103337.
3. Aydoğmuş, E., & Arslanoğlu, H. (2021). Kinetics of thermal decomposition of the polyester nanocomposites. *Petroleum Science and Technology*, 39(13–14), 484–500.
4. Aydoğmuş, E. (2022) Biohybrid nanocomposite production and characterization by RSM investigation of thermal decomposition kinetics with ANN. *Biomass Conversion and Biorefinery*.
5. Aydoğmuş, E., Dağ, M., Yalçın, Z. G., & Arslanoğlu, H. (2022). Synthesis and characterization of waste polyethylene reinforced modified castor oil‐based polyester biocomposite. *Journal of Applied Polymer Science*, 139, e525256.
6. Yanen, C., Dağ, M., & Aydoğmuş, E. (2022). Investigation of Thermophysical Properties of Colemanite, Ulexite, and Tincal Reinforced Polyester Composites. *European Journal of Science and Technology*, 36, 155–159.